**PCN 17\_0024 QUALIFICATION PLAN**

**OP400S AEROSPACE MODELS CHANGE OF FAB SITE & WAFER DIAMETER**

|  |  |  |
| --- | --- | --- |
| **TEST NAME** | **CONDITION** | **STATUS** |
| High Temp Operating Life Test | MIL-STD-883, TM1005  TA = +125C, 1000 Hrs. | Estimated Completion Date  4/1/2017 |
| Total Ionizing Dose (Radiation Hardness) | MIL-STD-883, TM1019  Condition A  3 Krads  10 Krads  30 Krads  50 Krads  100 Krads | Complete, All Pass |