Summary of results for QP#7143 for PCN 09-0094

The following list of qualification tests were completed per Qualification Plan #7143 for Gel Coat.   A qualification report will be provided once it is completed.

| Test | Conditions | Sample Size | Results |
| --- | --- | --- | --- |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 77 | Pass |
| Temperature Cycle* | JEDEC JESD22-A104 | 77 | Pass |
| Autoclave* | JEDEC JESD22-A102 | 77 | Pass |
| High Temperature Storage | JEDEC JESD22-A103 | 77 | Pass |
| Solder Heat Reflow | ADI-0049 | 33 | Pass |

*Preconditioned Per JEDEC/IPC J-STD-020