SMP04 Test Results

|  |
| --- |
| **QUALIFICATION RESULTS** |
| **Package** | **Die Attach** | **Mold Compound** | **Wire Type** | **Autoclave** | **HAST** | **HTS** | **Temperature Cycle** |
| 16L-SOIC | QMI519 | Hitachi Cel 8240HF10LX | Tanaka GLD Gold 1.3mils | Pass1  | Pass1 | Pass2  | Pass1 |
| 16-PDIP | Ablestik 84-1LMIS R4 | Sumitomo G600C | Tanaka GLD Gold 1.3mils | Pass1 | Pass1 | Pass2  | Pass1  |

1. Sample Sizes for test are 9 lots of 77 pieces for a total of 693 pieces
2. Sample Sizes for test are 3 lots of 77 pieces for a total of 231 pieces